CELL QUALIFICATION PROTOCOL

AUR-PR-340  —  Auriga Energy

| Document No. | CQP-AURPR340-00 |
| --- | --- |
| Target market | US / DOT |

1. Purpose

This protocol defines the qualification testing of the AUR-PR-340 cell manufactured by Auriga Energy, under IESF-4400. The cell is qualified across the following duty profiles: Aerospace Auxiliary.

2. Scope

Applies to the prismatic (hard-case) cell of chemistry LFP / Graphite. Testing is performed by Northgate Cell Qualification Laboratory (NCQL).

3. Reference Documents

Test Method Procedure: Test Method Procedure — AUR-PR-340

Acceptance Criteria & Limits: Acceptance Criteria & Limits (ACL) — AUR-PR-340

Vendor datasheet: Auriga Energy datasheet — AUR-PR-340

4. Test Article Description

| Manufacturer | Auriga Energy |
| --- | --- |
| Cell format | prismatic (hard-case) |
| Nominal voltage | 3.22 V |
| Charge voltage (max) | 3.65 V |
| Discharge cut-off (min) | 2.50 V |
| Rated capacity | 34.0 Ah |
| Storage condition | Storage condition: 25 °C nominal, 40 % SOC; do not store below −20 °C. |
| Supplied as | Delivered as hard-case prismatic modules, 12 cells per crate. |

5. Conditioning and Test Window

Each cell is conditioned by CC-CV charge to 3.65 V and discharge to 2.50 V. Cells whose graded capacity falls outside the band 33.40 Ah to 34.60 Ah are rejected before testing.

6. Duty Profile Test Matrix

Table 1. Duty profile test matrix.

| Sr. No. | Duty Profile | Conditioning Rate | Charge to | Discharge to | Cycles |
| --- | --- | --- | --- | --- | --- |
| 1 | Aerospace Auxiliary | 0.33C | 3.65 V | 2.50 V | 800 |
| 2 |  | 0.5C | 3.65 V | 2.50 V | 800 |

7. Qualification Test Parameters

7.1 Qualification Tests — Aerospace Auxiliary

| Sr. No. | Test Parameter | Acceptance Limit | IESF-4400 Clause |
| --- | --- | --- | --- |
| 1 | Capacity Verification | ≥ 97.0 % of rated capacity at 0.33C, 23 °C * $ | §6.2 |
| 2 | DC Internal Resistance (DCIR) | ≤ 18 mΩ at 50 % SOC, 25 °C # | §6.3 |
| 3 | Cycle-Life Endurance | ≥ 80 % capacity retention after 800 cycles $ | §6.4 |
| 4 | Insulation Resistance | ≥ 100 MΩ at 500 V DC | §6.5 |
| 5 | Overcharge Tolerance | No fire, no explosion at 1.5 × V_max charge @ $ | §6.7 |
| 6 | Forced Over-Discharge | No fire, no explosion; cell reversal limited to −0.50 V @ | §6.8 |
| 7 | Altitude Simulation | No leakage; ≤ 1.0 % capacity loss at 11.6 kPa / 6 h | §6.12 |

Acceptance Criteria:

All listed parameters meet the acceptance limits for this duty profile.

Conclusion:

The cell is qualified for this duty profile, subject to review.

Applicable notes from the ACL:

* Capacity limits apply to graded cells only; ungraded cells are assessed per IESF-4400 §6.2.1.

# DCIR is measured by a 10 s DC pulse at 1.0C and corrected to 50% SOC.

@ Mechanical-abuse limits apply to cylindrical and prismatic formats; pouch cells are governed by Annex P.

$ The test voltage window is defined by the cell vendor datasheet electrical ratings, not by this table.

Revision Record

| Revision | Date | Description | Author |
| --- | --- | --- | --- |
| 00 |  |  |  |